|  | VOSSLOH COGIFER POLSKA Sp. z o.o. |  |
| --- | --- | --- |
|  |  | Inst/GS/15/1 |
| Restoration of the surface profile of the turnouts by welding. |  |  |
| Izstrādāja: Karols Andžejevskis (Karol Andrzejewski) Inženieris metinātājs Pārbaudīja: #### Tomašs Vozņaks (Tomasz Woźniak) Inženieris metinātājs Datums: 11.08.2015. |  |  |
| Saskaņojumi: |  |  |

|  | VOSSLOH COGIFER POLSKA | INDEKSS: Inst/GS/15/1 |
| --- | --- | --- |
|  | Welding of steel DILLIDUR 400V | Date: 11.08.2015.g. |
|  |  | Page: 2/3 |

TABLE OF CONTENTS:

- Welding surface preparation.

- Preparation of additional welding materials.

- Heating before welding.

- Welding process.

- Grinding.

- Inspections.

- Additional requirements - compliance with existing norms and regulations.

- Preparation of the wear point of the groove base for proper repair process:

  - Preparation of the groove base - grinding to obtain a full flat surface of the groove;

  - Clean surfaces from rust, oils, greases, paints and other contaminants.

- Prepare additional welding materials:

  - Wire ESAB OK Tubrodur 15.43 - see informative map;

It is best to remove the wire from the original packaging before use.

Do not use damaged, unlabelled, rusted pre-opened packaging.

- the correct repair process of steel Dillidur 400V elements, they are heated to a certain temperature and the appropriate interlayer temperature is maintained within certain limits.

The repair site must be heated to 100-150 ° C with a burner. The temperature is controlled by

non-contact thermometer.

- The welding process must begin immediately after heating.

The process shall be performed over the entire width of the groove in parallel seams, in accordance with the attached pWPS / CP / 2015/1. The temperature must be controlled throughout the process. If the temperature drops below 100 0 C, it is essential to heat to the appropriate temperature.

- Grinding shall be carried out with equipment fitted with grinding wheels of a shape appropriate to the geometry of the groove to be repaired, in such a way as to obtain an appropriate height and width.

Grind to a straightness of 0.5 [mm] to 1 [m].

- VT tests shall be performed in accordance with PN-EN ISO 17637 and PT in accordance with PN-EN ISO 3452-1.

- Additional requirements:

  - Conditions for carrying out the process:

    - Ambient temperature: min. 10 0 C.

    - Humidity: max . 70%.

    - Wind speed: max . 1.5 m / s.

  - Up-to-date certificate PN-EN ISO 3834-2 for the company performing the welding process

|  | VOSSLOH COGIFER POLSKA IEKŠĒJIE MATERIĀLI | INDEKSS: Inst/GS/15/1 |
| --- | --- | --- |
|  | DILLIDUR 400V METINĀŠANA | DATUMS: 11.08.2015.g. |
|  |  | LAPPUSE: 3/3 |

- Qualified welding technology according to standards: EN ISO 15614, EN ISO 15613, EN ISO 15611 or EN ISO 15613.

- Up-to-date welder's certificate in accordance with PN-EN ISO 9606-1 (EN 287-1) - in the welding method used.

- Welding supervision according to PN-EN ISO 14731, min IWS.

- Test and study personnel in accordance with PN-EN ISO 9712, min. level 2.

- The temperature must be measured in accordance with PN-EN ISO 13916.

- Infrared thermometer with current calibration certificate.

- After grinding, carry out VT tests in accordance with PN-EN ISO 17637, quality class D in accordance with EN ISO 5817.

- After VT tests, perform PT tests according to PN-EN ISO 3452-1, acceptance level acceptance "3" according to PN-EN ISO 23277.

maģ. inž. Karols Andžejevskis

(mgr inż. Karol Andrzejewski)

##### PL – IWE – 00908 / 2011

inž. Tomasz Woźniak

(inż. Tomasz Woźniak)

##### PL – IWE – 00919 / 2011

PL/ IWI–C / 394 / 2013