# TECHNICAL SPECIFICATION FOR BOGIE FRAME INSPECTIONS

| No. | Technological Operation | Specific Requirements | Notes |
| --- | --- | --- | --- |
| 9.1. | Protective Covers for Components | The quantity and type of protective covers are specified in drawing 0833000078. | The Customer shall provide the protective covers indicated in the drawings for performance of the work. |
| 9.2. | Shot Blasting of Components | Complete removal of paint and metallization layers. After shot blasting, ensure surface roughness Ra ≤ 6.3 µm. | 1. Install protective covers, fasteners and cover the bogie frame according to 0833000078 page 1. 2. Covered surfaces shall not be damaged. 3. Processing shall not affect magnetic particle inspection results. |
| 9.3. | Magnetic Particle Inspection and Results | 1) Inspection areas: wheelset frame (drawing D0535327 MT): welded joints EN 1290/1291 level 2X; untreated casting EN ISO 9934-1 and EN 1369 quality level LM01, AM01, SM01; machined casting EN ISO 9934-1 and EN 1369 quality level LM001, AM001, SM001. 2) Inspection performed according to EN ISO 9712. A defect inspection report shall be prepared. Repair is possible where crack depth does not exceed 5 mm and length does not exceed 20 mm (3 mm in untreated casting). Grinding permitted no closer than 20 mm from welds. Maximum material thickness reduction: 10% of nominal thickness. | 1. Remove protective covers before inspection. 2. Inspection performed according to referenced standards or valid replacements. 3. A separate inspection report shall be prepared for each frame, indicating frame number and drawing. Any indication shall be shown on the drawing and accompanied by photographs. |
| 9.3.1. | Result: No indications detected | No unacceptable indications detected. | — |
| 9.3.2. | Result: Casting indications detected | Casting indications detected, removed by grinding, and no longer detected after repeat inspection. | Ground within permitted tolerances according to drawing DT112125=CP_1. Total permissible grinding depth: transverse 0.5–3.5 mm; vertical 1.0–5.0 mm depending on version I–VI. |
| 9.3.3. | Result: Unacceptable indications detected | Unacceptable indications remain after grinding; no further processing performed. | Frame returned to the Customer with inspection report attached. |
| 9.4. | Shot Blasting (Preparation for Metallization) | Before metallization, remove MPI residues and contamination by shot blasting to Sa2 (ISO 8501). | Install protective covers, fasteners and cover threads according to bogie frame drawing 0833000078 page 1. |
| 9.5. | Metallization | Perform metallization within 4 hours after shot blasting. Metallization thickness ≥80 µm. Material: zinc-aluminium 85/15 wire. | Install protective covers, fasteners and cover threads according to bogie frame drawing 0833000078 page 1. |
| 9.6. | Painting | Layer 1: 2K polyurethane primer, dry film thickness ≥90 µm, grey. Layer 2: 2K polyurethane paint, dry film thickness ≥80 µm, RAL 7021. | Install protective covers, fasteners and cover threads according to bogie frame drawing 0833000078 page 2. |
| 9.7. | Bogie Preparation for Shipment | Prepare inspection reports and handover documentation. Remove covers from untreated surfaces and preserve with Tectyl 506, CRC SP-400, Dinitrol 4941 or equivalent. | — |
| 9.8. | Documentation | Document confirming a 24‑month warranty. Summary of quality parameters of materials used (paint, galvanizing, protection class, metallization materials data). | — |