Appendix 1
TECHNICAL SPECIFICATION
Technical condition assessment and refurbishment repair of damaged Škoda 15T RIGA tram wheelset (bogie)

# 1. General Information and Purpose

To ensure continuous and safe operation of Skoda 15T RIGA trams (hereinafter referred to as the Tram), it is necessary to assess the technical condition of wheelset (bogie) frames and perform refurbishment repairs (hereinafter also referred to as refurbishment).

## 1.1. Subject Matter

| No. | Description | Catalogue Number | RS Nomenclature Number |
| --- | --- | --- | --- |
| 1. | Wheelset (bogie) frame | DO535327 | 0915020002 |

Technical parameters of the wheelset (bogie) frame:

| Parameter | Value |
| --- | --- |
| Manufacturer | SKD TRADE, a.s. |
| Dimensions (length/width/height) | 1713 mm / 910 mm / 450 mm |
| Base material | S355NL (GS20Mn6N) |
| Weight | 370 kg |
| Maximum axle load | 110 kN |
| Magnetic testing interval | 600,000 km or 10 years |

## 1.2. Characteristics of the wheelset (bogie) frames to be handed over under this contract

All frames handed over under this contract have an approximate mileage of 600,000 km, and damage has already been identified on each wheelset (bogie) frame. The defects are classified as follows:

| Defect Category | Description / crack location |
| --- | --- |
| A1 | Crack in casting, previously partially ground within permissible tolerance; crack still detectable after repeated testing |
| A2 | Crack in weld area |
| A3 | Crack in unmachined casting |
| B | Bearing seizure: mechanical damage to axle/seat |

Magnetic particle testing (MT) of wheelset (bogie) frames in defect categories A1, A2 and A3 has already been performed. The defect is known and confirmed by reports issued by an accredited institution, which are provided to the Contractor together with the frames submitted for repair.

For all defect categories, the Contractor shall perform a detailed assessment of the known defect and carry out repairs if the damage is potentially repairable.

If it is initially obvious that the damage is not repairable, the Contractor shall prepare a justified technical opinion declaring the frame unsuitable for repair without performing MT or geometry inspection.

The Customer shall specify the exact list of frames, identification numbers and defect categories in the handover report.

1.3. Scope, deadlines and warranty

Contract term: 2 years from signing. Orders are planned in batches of approximately 4-10 frames. Delivery time per order: up to 16 weeks.

Estimated total volume during contract term: approximately 30 frames. The Customer may submit fewer frames according to actual needs.

The Contractor shall provide a 24-month warranty for completed works, including anti-corrosion coating and repaired areas, from installation in the tram.

2. Scope of Work and Deliverables

2.1 General activities

- Inspection of the geometry of the wheelset (bogie) frames (see Clause 2.2).

- Magnetic particle testing inspection of the wheelset (bogie) frames (see Clause 2.3).

- Assessment of the technical condition of the wheelset (bogie) frames and evaluation of the identified damages.

- Preparation of a technical opinion for each wheelset (bogie) frame (repairable / non-repairable, with justification).

- If the Contractor determines that the wheelset (bogie) frame is repairable, the Contractor shall submit to the Customer a repair cost proposal for each wheelset (bogie) frame separately; the Customer shall evaluate the proposal and approve or reject the performance of the repair.

- Repair prices shall be determined in accordance with the Defect Category Prices.

2.2 Geometry inspection

Geometrical inspection shall be carried out for all submitted wheelset (bogie) frames that are subject to refurbishment, regardless of the category (A1, A2, A3 or B).

After surface cleaning (before any further works), the Contractor shall perform inspection of the geometrical dimensions, axle parallelism and seating dimensions of the wheelset (bogie) frames using a calibrated 3D measuring device or an equivalent method, based on the dimensions and tolerances specified in drawing DO535327.

The measurement results shall be recorded in the measurement report (see Section 5).

2.3 Magnetic testing

The Contractor shall have the right to use the MT reports provided by the Customer as an initial assessment. The scope of additional MT inspections shall be determined by the Contractor at its own discretion, if required for the preparation of the technical opinion. MT shall be performed for Category B defects if the defect is potentially repairable.

- The Contractor shall perform magnetic particle testing (MT) of the frame in accordance with the Customer’s Technical Specification No. [1] referred to in Section 3.

- Inspections may only be performed by personnel certified in accordance with the EN ISO 9712 standard.

3. Applicable Standards and Documentation

3.1. Standards

The following standards shall be applied for the non-destructive testing and repair of wheelset (bogie) frames:

- ISO/TS 18173 Non-destructive testing – General terms and definitions.

- EN 15085 (all relevant parts) – Welding of railway vehicles and components, including safety class CL1.

- EN ISO 17638 and EN ISO 23278 (level 2X) – Magnetic particle testing of welded joints.

- EN ISO 9934-1 and EN 1369 (quality grades LM01/AM01/SM01 and LM001/AM001/SM001) – Magnetic particle testing of castings in unmachined and machined areas.

- EN ISO 9712 – Qualification and certification of MT personnel (MT and VT, minimum Level 2, in the railway or mechanical engineering sector).

- EN ISO 9606 – Welder qualification testing.

- EN 1330-10 Non-destructive testing – Terminology – Part 10 – Terminology used in visual testing (VT – Visual Testing).

The Contractor may apply an equivalent international standard that ensures at least an equivalent level of quality and safety.

3.2 Customer technical specification

The magnetic particle testing methodology, surface preparation, assessment of acceptance criteria and requirements for application of the protective coating are specified in the Customer’s technical specification for bogie frame inspections (see Annex 1). The specification is based on the technical documentation of the tram manufacturer.

4. Repair

4.1. Repair conditions

The assessment of acceptance criteria and the subsequent minor grinding described in the technical specification referred to in Clause 3.2 of the Customer shall not be considered as repair of a defect.

The Contractor shall propose and justify its own technical solution that eliminates the identified defect and ensures at least an equivalent level of quality and safety compared to the original design. The Contractor shall assume full responsibility for the safety and suitability of the repair for operation.

If the Customer approves the cost proposal referred to in Clause 2.1, the Contractor shall ensure the following within the scope of the repair:

- compliance with the standards specified in Section 3 or their equivalents;

- a technological description of the repair process;

- a justification or calculation of the structural strength and safety;

- quality control and testing procedure;

- MT and geometrical inspection after repair (see Clause 4.3);

- preparation of documentation (see Section 5);

- a warranty for the performed repair works;

- confirmation of assuming responsibility for operational safety.

4.2 Additional requirements

If the Contractor proposes and performs the solution referred to in Clause 4.1 for the repair of the axle/bearing seat, the technical proposal and completion documentation shall additionally include:

- verification of the chemical composition of the axle material prior to any thermal treatment of the axle;

- a description of the applied procedure;

- confirmation of the compliance of the final geometry of the repaired functional surface, ensuring the possibility of installation of a new bearing/component, based on the dimensions and tolerances specified in drawing DO535327.

If deviations from the specified tolerances are identified as a result of the geometrical parameter inspection, the Contractor shall perform straightening, if technically feasible, ensuring compliance of the dimensions with the specified tolerances.

If defects are identified during repeated magnetic particle testing performed in accordance with the requirements of Clause 2.3, their technical assessment shall be carried out and the necessary repair shall be performed if the defect is potentially repairable.

4.3 Final inspections after repair

After completion of the repair specified in Clauses 4.1 and 4.2, and prior to the application of protective surface coatings:

- repeated MT inspection of the repaired areas as specified in Clause 3.2;

- repeated geometrical inspection as specified in Clause 2.2 to confirm full compliance with the manufacturer’s drawings and tolerances.

4.4 Surface protection

The surface protection process (metallization, priming and painting) shall be carried out in accordance with the Customer’s technical specification No. [1] referred to in Clause 3.2.

5. Documentation and Handover

Upon returning the frames after completion of the works, the Contractor shall indicate in the delivery note the frame identification numbers and the defect category specified in Clause 1.2.

5.1. Documents to be submitted for each wheelset (bogie) frame

- All previously mentioned inspection reports (Clauses 2.2, 2.3, 4.2 and 4.3);

- Technical opinion for each frame (Clause 2.1);

- Description of the repair technology (if repair has been performed);

- Confirmation of assuming responsibility for operational safety.

7. Transportation and Packaging

- The Contractor shall arrange and cover the transportation costs of the wheelset (bogie) frames to the repair location and delivery after completion of the repair to the Customer’s warehouse at Vestienas Street 35, Riga, or Tram Depot at Brīvības Street 191, Riga.

- The Contractor shall be responsible for the safe and proper packaging/securing of the wheelset (bogie) frames prior to their handover to the Customer, in order to eliminate the risk of damage to the restored anti-corrosion coating, paint coating or functional surfaces.

Appendices:

1. Technical Specification for Bogie Frame Inspections

2. Drawings